## Slide 1
1 Université de Lorraine, GREEN, F-54000 Nancy, France
2 Safran Tech, Electrical & Electronic Systems Research group, Rue des Jeunes Bois, Châteaufort, 78114 Magny-Les-Hameaux, France
3 Shibaura Institute of Technology ,3 Chome-7-5 Toyosu, Koto, Tokyo 135-8548 - Japan
Modelling of the pulsed field magnetization of a (RE)BaCuO bulk with a superconducting weld
*Rémi Dorget1,2, Kévin Berger1, Joseph Longji Dadiel3, Kimiaki Sudo3, Naomichi Sakai3, Tetsuo Oka3, Masato Murakami3 and Jean Lévêque1

## Slide 2
Top seeded melt growth
RE-Ba-Cu-O bulk welding process
Description of the model
Results

## Slide 3: Top seeded melt growth (TSMG)
Pellet of RE-Ba-Cu-O pressed then melted and slowly cooled to let the crystal grow
The seed crystal (RE-Ba-Cu-O with higher melting point) give the crystal orientation
  Examples of seed crystals : Nd-Ba-Cu-O or Sm-Ba-Cu-O
Several hours of oxygen annealing
Seed crystal
Growth sector boundaries
Growth sector regions

## Slide 4: Bulk welding process
Solder material: RE-Ba-Cu-O with low melting point
Process similar to TSMG: The solder material is melted while the bulk body act as the seed
Material | Tp [°C]
Y-Ba-Cu-O | 1008 °C
Er-Ba-Cu-O | 980 °C
Y-Ba-Cu-O + 10%Ag | 956 °C
Er-Ba-Cu-O + 10%Ag | 937 °C
Example of the temperature process for joining Y-Ba-Cu-O + 10%Ag with Er-Ba-Cu-O + 10%Ag
Good grain connection is obtain along the 110 plane

## Slide 5: Case study
Simulation of the weld behavior during pulsed field magnetisation (PFM)
Bulk body:
  Radius : 30 mm
  Height : 15 mm
  Homogeneous superconducting properties
Weld:
  Thickness : 1 mm
  Superconducting properties different from the bulk body
Objective: study the magnetisation for different welds
Weld
Bulk body

## Slide 6: Simulated setup
Welded bulk
Magnetising coil
Cryostat
Cold head
Initial temperature : Ta = 60 K
Cryocooler cooling power : Pcryo = 50W
Applied magnetic field : Ba = [0.5 T : 9 T]

## Slide 7: Electromagnetic and thermal models
3-D Electromagnetic model
3-D Thermal model
z
x
y
z
x
y

## Slide 8: Electromagnetic model
H-formulation
:
  In the bulk body :
  In the weld:
  Weld to bulk body critical current ratio:

## Slide 9: Simulation parameters
Due to symmetries → ¼ of the geometry is simulated
Parameter | Value | Description
 | 300 A/mm2 | Self field critical current density at 77 K
 | 0.5 T | Magnetic field dependance constant
 | 1.2 | Magnetic field dependance exponent
 | 20 | n exponent at 77 K and B = 0 T
 | 6 | n exponent at 77 K and B >> B0
 | 92 K | Critical temperature
 | 77 K | Reference temperature
 | 60 K | Initial temperature
 | [0.5 T : 9 T] | Applied flux density
 | 10 ms | Pulse time constant
 | [0.25 : 1] | Weld to bulk body critical current ratio
 | 50 W | Cooling power of the cold head
 | 6 g/cm3 | RE-Ba-Cu-O density
 | 150 J/(kg.K) | Heat capacity
 | 5 W/(m.K) | Thermal conductivity
Parameter | Value | Description
 | 300 A/mm2 | Self field critical current density at 77 K
 | 0.5 T | Magnetic field dependance constant
 | 1.2 | Magnetic field dependance exponent
 | 20 | n exponent at 77 K and B = 0 T
 | 6 | n exponent at 77 K and B >> B0
 | 92 K | Critical temperature
 | 77 K | Reference temperature
 | 60 K | Initial temperature
 | [0.5 T : 9 T] | Applied flux density
 | 10 ms | Pulse time constant
 | [0.25 : 1] | Weld to bulk body critical current ratio
 | 50 W | Cooling power of the cold head
 | 6 g/cm3 | RE-Ba-Cu-O density
 | 150 J/(kg.K) | Heat capacity
 | 5 W/(m.K) | Thermal conductivity

## Slide 10: Results – Field maps
Penetration of the magnetic field during a 4 T pulse Top: α = 1 Bottom : α = 0.5
Trapped field map after 60 s

## Slide 11: Results – Trapped flux
Trapped flux on the bulk surface:
Above 2 T → weld reduces the trapped flux
Below 2 T → weld increases the trapped flux (up to 13 %)

## Slide 12: Conclusion
A superconducting weld with a reduced critical current help the magnetic field to penetrate the bulk
  Increased trapped flux at low applied field
  Decreased trapped flux at high applied field
  → Applications with small inductor coil (magnetisation from armature windings)
The solder can be doped to improve its thermal properties at the expense of the magnetic properties

## Slide 13
Rémi Dorget,  (+33) (0)6 82 52 22 86,  e-mail: remi.dorget@univ.lorraine.fr
Thank you for your attention