## Slide 1: 2D Numerical Simulations of HTS Stacks of Tapes for Cable-in-Conduit Conductors
Gianluca De Marzi, ENEA
7th International Workshop on Numerical Modelling of High-Temperature Superconductors
22nd-23rd June 2021
Virtual (Nancy, France)

## Slide 2: Introduction
Cable-in-conduit conductors comprised of twisted stacks of HTS tapes with aluminium slotted core constitute a very promising technology by virtue of their easy manufacturing process, flexibility capabilities, and high current densities. Currently, applications in the nuclear fusion industry of this HTS cable concept are being considered for the improvement of DTT and DEMO reactor performances.
jacket
HTS stack
Al core
Tiles
FBG sensor
He channel

## Slide 3: Aim
In a cable, the current distribution among tapes is one of the key parameters affecting the cable performances
We here present a 2D finite-element model, which computes the magnetic field and current distribution in stacked tapes
This model can be also used to describe the experimental V-I results obtained in cables in which different current distributions among tapes are expected.

## Slide 4: Methodology
A is defined all over the bounded universe, while T is exclusively defined along the superconducting medium
Thin strip approximation: the superconducting tapes are modeled as 1D objects
Transport currents are applied by a proper choice of the boundary conditions for T:
T-formulation
A-formulation
T = Tn
K
The T-A formulation of the Maxwell's equations is a well-established model, and it has already been applied to a variety of HTS devices, such as coils and cables

## Slide 5: Cable’s Termination Resistances
The model includes the termination resistances
This approximation is valid when tape-to-tape contact resistance is higher than the tape termination resistance as likely occurs for lab-scale samples
Equivalent circuit models:
(a) single stack; (b) two stacks

## Slide 6: Critical Current: Angular and Field Dependence
The model includes the Ic(µ0H, ϴ) dependence
The experimental lift factors, are globally fitted to the abovementioned equation using the Igor Pro’s Global Fit package with Ic0, ɡ, α, and β as global parameters and the flux density B as a local parameter.
B
ϴ
tape

## Slide 7: Magnetic fields and currents
Left: Field map for the single stack. The direction and relative magnitude of the current vector potential T is plotted for two selected tapes, one on the top and the other in the middle of the stack. Right: field map for two adjacent stacks.
Magnetic field calculated with the T-A formulation close to the S-N transition region

## Slide 8: Experiment #1: Stack of 20 THEVA Tapes
Cu-stabilized tape Pro-Line TPL4300c, by THEVA, has been used (Table I). The investigated 1-m-long CICC sample is comprised by one stack of 20 HTS tapes and four dummy stacks of Stainless Steel (SS) tapes.
Table I Experiments #1 and #2: main parameters of the HTS tape and CICC cable (w = width; t = thickness). | 
Parameter | Sample
HTS tapea Tape size (w x t) [mm x mm] Substrate, thickness [mm] Cu stabilizer’s thickness [μm] Ic [A], 77 K self-field Twist pitch [mm] Core diameter [mm] Number of slots Slot size (w x h) [mm x mm] Number of HTS stacks Number of tapes per HTS stack Number of dummy stacks Dummy tape, (w x t) [mm x mm] | THEVA TPL4300c 3.4 x 0.15 Hastelloy C-276, 0.1 20 (per side) ~160 ∞ 19 5 4.3 x 4.3 1 (Exp. #1), 2(Exp. #2) 20 4 (Exp. #1), 3(Exp. #2) SS, 4.0 x 0.15
a From Datasheets provided by supplier. | 

## Slide 9: Experiment #1: Stack of 20 THEVA Tapes
Individual tape current as a function of cable current. Left side: Rterm is equal for all tapes in the stack: (a) 1 nΩ; (b) 10 nΩ; (c) 100 nΩ; (d) 500 nΩ; Right side: gaussian distributed random values of Rterm, with standard deviations of: (a) 32 nΩ; (b) 261 nΩ.

## Slide 10: Experiment #1: Stack of 20 THEVA Tapes
Individual tape current as a function of cable current. Left side: Rterm is equal for all tapes in the stack: (a) 1 nΩ; (b) 10 nΩ; (c) 100 nΩ; (d) 500 nΩ; Right side: gaussian distributed random values of Rterm, with standard deviations of: (a) 32 nΩ; (b) 261 nΩ.
For I « Ic, the current repartition is governed by the Rterm values and the inductance distribution among tapes, whereas self-field effects become dominant for I ⪅ Ic
In spite of Rterm variations by more than two orders of magnitude, the shape of the E-I characteristic curve of figure 3 does not change.

## Slide 11: Experiment #2: Two Adjacent Stacks of THEVA Tapes
The critical currents of the stacks differ by about 50 A. This can be explained in terms of different superconducting properties of the two stacks (i.e., different <Ic> and <n>) and by a reduced current sharing between the two stacks.
To study the current distribution among different stacks within the CICC, we made a second cable very similar to the one used in Exp. #1, using the same THEVA tapes.

## Slide 12: Experiment #3: Stacks in a Bent Cable
To study the effect of the variation of Ic among tapes, we have analyzed the current distribution in a 1-meter cable which has been bent down to Rb = 0.15 m.
Table II Experiment #3: main parameters of the HTS tape and CICC cable (w = width; t = thickness). | 
Parameter | Sample
HTS tapea Tape size (w x t) [mm x mm] Substrate, thickness [mm] Cu stabilizer’s thickness [μm] Average Ic [A], 77 K self-fielda Twist pitch [mm] Core diameter [mm] Number of slots Slot size (w x h) [mm x mm] Number of tapes per HTS stack Dummy tape, (w x t) [mm x mm] Wrapping tape, (w xa t) [mm x mm] External jacket, thickness [mm] | SuNAM SCN04150 4.0 x 0.15 Stainless steel, 0.1 20 (per side) 245 500 19 5 4.3 x 4.3 20 SS, 4.0 x 0.15 40 x 0.1 Al tube, 1.25
a From Datasheets provided by supplier. | 
Each tape has been measured individually; large Ic variations among tapes is found.

## Slide 13: Experiment #3: Stacks in a Bent Cable
Individual tape current as a function of cable current for three different value of Rterm: (a) 10 nΩ; (b) 100 nΩ; (c) 500 nΩ.
Measured E–I curve of the 20-tapes SuNAM stack (open circles). Continuous and dotted lines represent the FEM solution and the fit to the power law, respectively.

## Slide 14: Experiment #3: Stacks in a Bent Cable
Individual tape current as a function of cable current for three different value of Rterm: (a) 10 nΩ; (b) 100 nΩ; (c) 500 nΩ.
Measured E–I curve of the 20-tapes SuNAM stack (open circles). Continuous and dotted lines represent the FEM solution and the fit to the power law, respectively.
Some of the tapes have been damaged by bending and showed degradation.
They therefore entered the current sharing regime well before the transition to the normal phase of the whole stack
Consequently, the current distribution was highly uneven. In spite of this, the stack showed good electrical stability.

## Slide 15: Experiment #3: Stacks in a Bent Cable
Individual tape current as a function of cable current for three different value of Rterm: (a) 10 nΩ; (b) 100 nΩ; (c) 500 nΩ.
Measured E–I curve of the 20-tapes SuNAM stack (open circles). Continuous and dotted lines represent the FEM solution and the fit to the power law, respectively.
Such an unbalanced current sharing might generate thermal instabilities well below the transition, thus increasing the risk of catastrophic damage of the superconducting cable. Largely uneven Ic distributions should always be avoided.

## Slide 16: Perspectives
This model can also be useful for predicting the performance of a fully equipped HTS CICC in self-field conditions, and can be used for design and development activities of superconducting cables based on HTS coated conductor tapes.
Next step will be to implement a full 3D model to predict the behavior of a current-carrying HTS twisted stacked-tape CICC in an external magnetic field, as in typical operating conditions of a nuclear fusion reactor.

## Slide 17
gianluca.demarzi@enea.it
With kind contributions by:
Andrea Augieri
Giuseppe Celentano
Marcello Marchetti
Angelo Vannozzi