## Slide 1: Fast and efficient HTS modelling using ANSYS A-V formulation
Kai Zhang :: Insertion Device Group :: Paul Scherrer Institute
SLS 2.0
7th International Workshop on Numerical Modelling of High Temperature Superconductors
23.06.2021, Virtual (Nancy, France)
Acknowledgement: Mark Ainslie (Cambridge), Lucas Brouwer (LBNL), Ryota Kinjo (RIKEN Spring-8), Marco Calvi, Thomas Schmidt and Sebastian Hellmann (PSI)

## Slide 2: Outline
HTS for undulator applications
HTS modelling using ANSYS A-V formulation
      Resistivity-adaptive algorithm (RAA)
              Critical state model: 2D
      Direct iteration method
              Flux creep model (E-J power law): 2D and 3D
              Critical state model: 2D
      Backward computation method
              Critical state model: 2D and 3D
Conclusion

## Slide 3: PSI Light sources: Storage Rings and FELs
undulator
undulator
Storage Rings
Free-Electron Lasers

## Slide 4: SwissFEL, Aramis beamline (PM undulator)
15mm period
3mm gap
B0 = 1.28T
3500 periods
40m long
In future, we want to go to 10mm period …

## Slide 5: Staggered-array bulk Re-Ba-Cu-O undulator
@6K
10mm period & gap = 4mm
GdBCO Bulks
R.Kinjo et al. Appl.Phys. Express 6 (2013)
Ideally, By can reach 2T when ∆𝐵𝑠 = 10T.
This HTS undulator concept is attractive to the new hard x-ray beamlines planned for both SLS2.0 and SwissFEL at PSI.
Kinjo R et al 2008 Proc. 30th FEL Conf. 473-76

## Slide 6
@6K
10mm period & gap = 4mm
Our big Challenge is large-scale HTS magnetization simulation and optimal
design of the magnetic field (fast simulation desired)
ANSYS

## Slide 7: A: Resistivity-Adaptive Algorithm (RAA)
First proposed by Hidetoshi Hashizume et al in 1992
    Initial electric-conductivity of all HTS elements is assumed sufficiently large
    If , then
Further developed by Chen Gu et al in 2005 and 2013, and by Stefania Farinon et al in 2010 and 2014 through using ANSYS Parametric Design Language (APDL)
    Initial resistivity of all HTS elements is set to a low value
    Update , until for all HTS elements
Hashizume H et al 1992 IEEE Trans. Magn. 28 1332-35
Gu C and Han Z 2005 IEEE Trans. Appl. Supercond. 15 2859-62
Farinon S et al 2010 Supercond. Sci. Technol. 23 115004
Farinon S et al 2014 Supercond. Sci. Technol. 27 104005
Gu C et al 2013 IEEE Trans. Appl. Supercond. 23 8201708

## Slide 8: A: RAA – Screen currents
Iop = 1060A Iop = 0A
JZ (A/m2)
JZ/Je
On the left is the simulated screen currents inside a periodical FEA model (transport current Iop ramps to 1060A and drops to 0A).
The rigorous critical state in the outer layer can still be reached during Iop drops, but there is a slight decay in the inner layer (this issue was also emphasized in [Gu C. et al 2013] and remained to be solved).
Computation speed: ~5 min for 60000 DOFs
1
-1

## Slide 9: A: RAA - Cylindrical bulk superconductor
Trapped JZ after ZFC magnetization from 0 to 1T, Je=3e8 A/m2
ANSYS(RAA), critical state COMSOL(E-J power law), n = 100
Inconsistent critical state magnetization currents are found in ANSYS and COMSOL models, further examination with backward computation method proves the COMSOL result is correct.
It is still unclear why the RAA method fails in modelling the bulk superconductor ? Only feasible for transport current cases ? More research studies are required to address this problem …

## Slide 10: B: Direct iteration method
  Initial resistivity of all HTS elements is set to a low value;
  The whole magnetization process is divided into N steps;
  For simulating the flux creep model, resistivity of each HTS element is updated after every iteration
  For simulating critical state model, each penetrated HTS element is forced with the latest Jc after every iteration
reservation coefficient, usually quite large

## Slide 11: B: Direct iteration method (E-J power law, 2D)
JZ in the magnetized bulk HTS (n = 20) at (a) t = 500 s, (b) t = 1000 s and (c) t = 1500 s from using ANSYS A-V formulation;
JZ in the magnetized bulk HTS at (d) t = 500 s, (e) t = 1000 s and (f) t = 1500 s from using COMSOL H-formulation.
Applied magnetic field versus time
Zhang K et al 2021 IEEE Trans. Appl. Supercond. 31 6800206
Related APDL codes are shared in
https://www.researchgate.net/profile/Kai-Zhang-32

## Slide 12: B: Direct iteration method (E-J power law, 3D)
A/m2
A/m2
A/m2
JX
JY
JSum
Trapped current in a ¼ half-moon shaped bulk superconductor model after FC magnetization from 8T to zero (Je = 1e10 A/m2, n = 20)
Problems: a number of iteration steps (usually >200) are essential to obtain smooth E-J power law based simulation results, this might result in a large amount of computation time for complex 3D FEA model.

## Slide 13: B: Direct iteration method (critical state model, 2D)
(a) FC magnetization of the ReBCO tape stack; (b) 2D axis-symmetric half FEA model.
(a) Trapped Bs, (b) flux lines, (c) Jz, and (d) hoop strain in the ReBCO tape stack after FCM from 10 T.
Zhang K et al 2020 IEEE Trans. Appl. Supercond. 30 4700805
Related APDL codes are shared in
http://www.htsmodelling.com/ (model #23)

## Slide 14: C: Backward computation method
Ideal: HTS bulk acts as a permanent magnet after FC magnetization.
Reality: this situation can never be realized since the flux pinning force is always limited.
Assuming HTS bulk is FC-magnetized under isothermal conditions,
eddy currents will gradually penetrate inwards
following a quasi-static critical state model.

## Slide 15: C: Backward computation method Critical state model – 2D
Algorithm for the backward computation method for computing the critical state in a field-cooled magnetized bulk superconductor.
Critical state after FCM from 10T
(with minimum electro-magnetic entropy production [Pardo E 2017 J. Comput. Phys 344 339-63])
Trap >10T field after introducing an additional penetration layer
One more penetration layer

## Slide 16: C: Backward computation method Critical state model – 3D
Schematic of 1/4 cuboid bulk

## Slide 17: C: Backward computation method FEA model of 3D bulk HTS undulator
Number of DOFs: 6.5 million !

## Slide 18: C: Backward computation method Modelling of 3D bulk HTS undulator
Magnetic field component Bz and the magnetization current density Js in the BHTSU obtained using the A-V, H and H-φ [see A. Arsenault’s talk] formulations
Magnitude of Js in the central HTS bulk in the xy-plane. “z = 0” refers to the mid-plane of the HTS bulk; “z = 2 mm” refers to the outer surface of the HTS bulk.
ANSYS
COMSOL
COMSOL
ANSYS
COMSOL
COMSOL

## Slide 19: C: Backward computation method Modelling of 3D bulk HTS undulator
 |  | No. of DOFs (million) | Computation time (hour)
ANSYS | A-V (backward computation) | 6.5 | 12.5
COMSOL | H | 3.2 | 151
COMSOL | H-φ | 1.3 | 23
Zhang K et al 2021 arXiv:2105.01761
Related APDL codes and COMSOL models will be shared soon in
http://www.htsmodelling.com/
Comparison of the calculated on-axis undulator field obtained using the A-V, H and H-φ formulation models
Summary of computation times for the ten-period bulk HTS undulator

## Slide 20: C: Backward computation method Optimal design of bulk HTS undulator
(a) Side view of the optimized BHTSU; (b) End view of the optimized BHTSU; (c) Vector sum of the magnetization current density in the simplified BHTSU model; (d) Undulator field By along z-axis;

## Slide 21: C: Backward computation method Optimal design of bulk HTS undulator
(e) First integral of the undulator field IBy along z-axis; (f) Second integral of the undulator field IIBy along z-axis.

## Slide 22: Conclusion
Three numerical algorithms implemented in ANSYS are benchmarked with COMSOL H/H-φ formulation.
The RAA method shows fast computation of the screen currents in HTS coils charged with transport current; problems are met for simulating bulk superconductors.
The direct iteration method can solve magnetization problems for both flux creep model (E-J power law) and critical state model, and for both 2D & 3D; the critical state solution is fast while the flux creep solution is slow (a large amount of iteration steps are required).
The backward computation method shows extremely fast computation speed in modelling the critical state in large-scale (6.5 million DOFs) bulk HTS undulator model for both 2D & 3D (important for optimal design).
ANSYS is quite flexible for secondary development; most of the HTS magnetization or multi-physics coupled problems can be solved efficiently by using the above mentioned numerical algorithms.

## Slide 23
We are delighted to share our APDL codes and stimulate the ANSYS community in HTS modelling !
The APDL codes for both the RAA and the direct iteration method have been shared on the HTS modelling workgroup (#19, #23); the APDL codes for the backward computation will also be shared on the webpage soon.
Contact： kai.zhang@psi.ch

## Slide 24: Extra - Backward computation method
;
Magnetization current JT in the periodical HTS bulk undulator during the backward iterations
Magnetization current JT in the periodical HTS bulk undulator solved using COMSOL H-formulation
Zhang K et al 2020 SUST 33 114007
Ainslie M et al 2016 SUST 29 074003
Trillaud F et al 2018 IEEE TASC 28 6800805
[Trillaud F et al 2018]
[Ainslie M et al 2016]

## Slide 25: Extra - Backward computation method
Zhang K et al 2020 Supercond. Sci. Technol. 33 114007
Comparison of computation times reported in the literature for other state-of-the-art techniques for the electromagnetic analysis of HTS materials.
Note: the listed H-, T- and T-A formulation were implemented for other applications (e.g., AC loss or SCIF) and that benchmarking this particular problem would provide a true comparison.