## Slide 1
SCS4050
Analysis of contact behavior in CORC® cabling and under axial tension
K. Wang1, 2, V. A. Anvar1, 3, Y. Gao2, J D Weiss4, D.C. van der Laan4, A. Nijhuis1
1The University of Twente, Faculty of Science & Technology, 7522 NB Enschede, Netherlands, 2 College of Civil Engineering and Mechanics, Lanzhou University, 730000 Lanzhou, China, 3Institute for Superconducting and Electronic Materials, University of Wollongong, Wollongong, Australia,
4Advanced Conductor Technologies and University of Colorado, Boulder CO 80301, USA,
Abstract
CORC® cables or wires are composed of helical wound HTS REBCO tapes in multiple layers with high flexibility. In this study, starting with the cabling process, the deformation of the tape and the initial contact force distribution between the tape and the core are described. Then axial tensile loading of the CORC® is simulated and compared with the experimental curve including its critical current degradation. The results describe the interaction between tape and core that occurs during the tensile loading. The tape and the core are extruded and friction is generated, directly causing critical current degradation. The developed analytical and FE models can predict the mechanical and electrical properties of CORC® cables.
Conclusions
The contact behavior of CORC® cable is studied in FE model and theoretical method.
A CORC® axial tensile model was built. The tape strain, normal contact stress and friction force were calculated.
The electromagnetic analysis model of CORC® cable considering the tape deformation and interlayer contact during cabling process, cooling process and axial tensile loading process was established. The validations are ongoing.
CORC cabling process
Pitch and core radius：
Radius of curvature：
Average one layer contact force:
+ +..+
Cooling process
 | 17.7e-6 | 1/K
 | 13e-6 | 1/K
 | 77 | K
 | 293.15 | K
 | 17.7e-6 | 1/K
 | 13e-6 | 1/K
 | 77 | K
 | 293.15 | K
Poster id: htsmod2020:350772
Lanzhou University
Approximate average contact force:
Edge Lifting affects depth of the tape edge:
test data [1]
Linear hardening model
test data [1]
Idea plastic model
-
[1]D C van der Laan, D M McRae and J D Weiss, Effect of monotonic and cyclic axial tensile stress on the performance of superconducting CORC® wires. Supercond. Sci. Technol. 32 (2019) 054004
A side：
no relaxation
B side：relaxation
Multilayer CORC cabling process
Tape thickness t [mm]
Tape Width w [mm]
Core radius r [mm]
Winding angle [°]
Tape Tension F [N]
Contact pressure define(MPa)
Apply contact pressure(Pa)
Tape selection
Winding method
Tension model considering Initial Contact
0 MPa initial contact pressure
5 MPa initial contact pressure
Theory of CORC tension process
Approximated as:
Helical angle (r=1.29 mm, w=2 mm, =0.3, =0.3, )
Friction force
The friction is the largest at the edge and the least in the middle.
The direction of friction is different from the tape axis.
3D T-A method for CORC tension process consider contact behavior
Step-1 solid:
Calculate the overall strain of the cable
Step-2 shell:
Calculate the strain in the REBCO layer
Step-3 T-A
Calculate the critical current, current distribution, magnetic field, AC loss and other electric behavior
1. T-formulation
2. A-formulation
Base equation
3. Power law
4. AC & DC applied current
and magnetic field
AC
DC
Case 1. When there is no background magnetic field, only DC transport current.
Transport current distribution [A/m2]
0.5%
1.0%
1.5%
2.0%
Critical current degradation Jc/Jc0 [1]
2-layers tensile CORC results (cable strain: 1%, winding angle：45°-45°, core radius：1.29 mm)
Step-1 solid
Tape axial strain
Step-2 shell
REBCO axial strain
Case 2. When there is no transport current, only the current generated by the background magnet.